# Web Site changes 030710

## New Properties data

PocoFoam

Emissivity (can also be used as an estimate of solar absorptivity) = 0.62 (Poco)

=  0.778 (Space Systems Loral)

Outgassing: 	Total Mass Loss (TML)- based on ASTM E-595 = 0.031%

Volatile Content matter (VCM) )- based on ASTM E-595 = 0.017%

(Data from Space Systems Loral)

## PocoFoam/ Carbon Fiber sandwich panel construction and properties

Composite Optics, Inc. fabricated a sandwich panel using PocoFoam as the core and carbon fiber epoxy as the facesheets.  These were tested in shear loading of the core, compression of the core (Core Face Wise Compression - FWC) and skin (Sandwich Edge Wise Compression - EWC).  Tension samples were tested (Sandwich Face Wise Tension- FWT). Data provided by Composite Optics, Inc. for PocoFoam epoxy bonded between carbon fiber facesheets.

| Test | Average Value | Failure Mode |
| --- | --- | --- |
| Core Shear |  |  |
| Modulus | 164 Ksi | Core Failure |
| Strength | 242 psi |  |
| Core Face Wise Compression |  |  |
| Modulus | 18 Ksi | Core Crush |
| Strength | 412 psi |  |
| Sandwich Face Wise Tension |  | Core Failure |
| Strength | 490 psi | (No Adhesive Failure) |
| Sandwich Edge Wise Compression |  |  |
| Modulus (Skin) | 24 Msi | Facesheet Buckling |
| Strength | 20 Msi |  |

## Physical properties as reported by “Round Robin Tests of Carbon Foam Mechanical Properties” Alan Landis, Sangwook Sihn, Ajit Roy, Air Force Research Laboratory (AFRL-ML), Proceedings of the 4th AFRL Carbon Foam Workshop, 2002.

| Physical Properties |  |  |  |
| --- | --- | --- | --- |
| as measured by AFRL- |  |  |  |
|  |  |  | PocoFoam |
| Density |  | lb, ft^3 | 28.3305 |
|  |  | g/cc | 0.45 |
| Compressive Strength |  |  |  |
|  | x-y | psi | 259 |
|  | z | psi | 380 |
| Stiffness |  |  |  |
|  | x-y | ksi | 25.179 |
|  | z | ksi | 51.3 |
| Torsion Shear |  |  |  |
|  | Avg. Strength | psi | 265 |
|  | Avg. Stiffness | ksi | 63.518 |

## Shown below is the comparison of the compressive behavior of PocoFoam and Poco-HTC.  The PocoFoam behavior is typical of foams in general.  The Poco-HTC is typical of the behavior of porous solids.

## CTE – See Charts below.

Samples were measured on a Netzsch Model 402C Dilatometer.  Up-heat rate was 10°K/min. in argon atmosphere.  The figures show that both POCO Thermal Management Materials expand differently in the growth (z-axis) compared to the plane of the billet (xy plane).  The charts show Expansivity data, which gives an accurate representation of the material expansion behavior over temperature range.  The table of CTE values is taken as the slope of the expansivity curves between the temperature of interest and the reference temperature (30°C).

## Thermal Conductivity – See Chart

## Pressure drop

### Upper use temperature

450°C ( 842°F) in air

2500°C (4532°F) in vacuum or inert gas atmospheres

### Graphite d-spacing

| Sample | HTT °C | d-spacing. (A) | 2-Theta, degrees |
| --- | --- | --- | --- |
| Poco-HTC | 2870 | 3.3682 | 26.440 |
| PocoFoam | 2800 | 3.360 | 26.4 |

### Specific Surface Area

(estimated by Wirtz, et.al. at University of Nevada-Reno)

( (beta) = 5,000-10,000 m^2/m^3

## Contract Awardees

Recent efforts sponsored by various government contracts are paving the way to understanding these new materials. evaluation of devices utilizing  PocoFoam and Poco-HTC.  The following is a partial listing of contracts that are evaluating the POCO materials.

| Title | Company | Contact/ link |
| --- | --- | --- |
| Thermal Panels for Spacecraft | Northrop-Grumman |  |
| Deep Space Concentrator Mirror | Composite Optics, Inc. |  |
| Phase Change Cooling for Space Based Radar | Thermal Management & Materials Technology | TMMTdrv@aol.com |
| Aircraft Heat Exchanger | Allcomp |  |
| Phase Change Cooling Device | University of Nevada – Reno |  |
| Attachment for Electronics Cooling | Materials Resources International | www.s-bond.com |
| Copper filling of Carbon Foam | Thermal Management & Materials Technology | TMMTdrv@aol.com |

# 2003 SBIR Contracts utilizing Poco Thermal  Management Materials

| Title | Company | Contact/ Link |
| --- | --- | --- |
| High Strength Aircraft Heat Exchangers | Allcomp/ TMMT | TMMTdlv@aol.com |
| Hybrid Thermal Protection System | TMMT | Same |
| Active Radar Thermal Management | TMMT | Same |
| Foam/ Cu Composite for Electronics | TMMT | Same |
| Ballistic Missile Composite Structures | Ceramic Composites | cduston@techassess.com |
| Foam Heat Exchanger for Power Plant Cooling | Ceramic Composites | cduston@techassess.com |
| Ballistic Missile Innovative Propulsion Products | Advanced Ceramics | mplatero@acmtucson.com |