## Tube Bending Trials for Prototype ATLAS Upgrade Stave

### Annealing

Aluminum 3003 tubing ID/OD(8/8.7 mm) is used and hand annealed using a heat gun.

Bending

### Flattening

Shim size is 0.284”

### Results

After flattening.

| Sample | Anneal T(oF) | Bead Filled? | Thickness(inches) | Width(inches) |
| --- | --- | --- | --- | --- |
| 1 | 850 | yes | 0.292-0.295 | 0.368-0.371 |
| 2 | 1030 | yes | 0.292-0.294 | 0.365-0.374 |
| 3 | 1000 | no | 0.287-0.291 | 0.367-0.385 |
| 4 | 850 | no | 0.287-0.289 | 0.365-0.385 |