# IC Wafer Thinning

## Introduction

The design goal for the thickness of the front-end electronics is 150 microns. The prototype work so far has used mechanical thinning of the integrated circuit(IC) wafers after deposition of the bumps on the IC wafers. Dummy wafers and a few active wafers have been thinned successfully. Bumped wafers processed by Boeing, AMS, IZM and Sofradir have been thinned. The bumps on the IC wafers are protected by a layer of photoresist. Additional protection is provided by  tape applied to the active side(photoresist side) of the wafers. This tape is removed by the thinning vendor after thinning, leaving the photoresist on the thinned wafers. The thinned wafers are inspected by the vendor(a quick visual inspection and the thickness of each wafer is measured). Additional QA must be provided by ATLAS.

## Prototype Results

We have prototype experience with wafers processed by four bump bonding vendors: Boeing(no longer active), AMS, IZM and Sofradir. We summarize below our experience with mechanical thinning with each of these sources of bumped wafers. We have also tried non-mechanical thinning(plasma thinning) but this is currently not planned to be used in production. The flip-chip-defect rate(ie. merged or missing bumps) is not yet well measured for thinned ICs with any of the vendors, although all vendors have made  thinned dummy and/or active modules. We need more modules to have a better estimate of the defect rate, particularly the difference, if any, between thinned and not-thinned die.

### Boeing

One-half of a 6" FE-B wafer was ground successfully by GDSI to 150 microns thickness after indium bump deposition by Boeing. This wafer was diced and a 16 chip module made with good success. Boeing subsequently abandoned bump bonding for external customers.

### Alenia Marconi Systems(AMS)

Dummy 4" wafers and active IC wafers(6") bumped by AMS have been thinned by Okamoto. The thickness results to date are summarized in Table 1. The target thickness is specified as a minimum. The vendor accuracy is approximately ( 10 microns.  The indium bumps deposited by AMS are protected by a thin layer of photoresist(5-10 microns thick). The photoresist-surface of these wafers is covered by UV-releasing tape. Two dummy modules have been very recently assembled and are under test. Two active modules have been assembled and tested.3 AMS so far observes little qualitative difference in the bump yield after thinning(i.e. no significant damage) but is just now making the first accurate measurement of this yield, including die lost in handling.

| Wafer Type(s) | Target Thickness(() | Measured Thickness(() |
| --- | --- | --- |
| 4" dummy(4 wafers) | 152(+25, -0) | 165-166 |
| Active(Wafer 11)(6") | 152(+25, -0) | 156 |
| Active(Wafer 15)(6") | 165(+25, -0) | 171 |

Table 1. Wafer thinning results with Alenia Marconi Systems.

### IZM

Dummy 6" wafers bumped by IZM have been thinned by Okamoto. No active wafers have yet been thinned(although this will occur soon). The process used is identical to that employed for the AMS-bumped wafers. However, the photoresist thickness protecting the bumps has been significantly thicker(about 30 microns) in the wafers received to date. Non-uniformities(eg. edge bead) in the photoresist create problems in the grinding. As the silicon is thinned, it become too weak and the wafer cracks(if the edge bead is higher than the rest of the wafer) and cracks or chips are created at the edges of the wafer(if the edge bead is lower than the rest of the wafer). The protective tape can reduce these effects, and a thicker tape than for AMS-bumped wafers was used for IZM wafers. So far we have successfully thinned four IZM-bumped wafers to about 200-210 microns with their current photoresist processing. Thinner wafers appear feasible if the thickness of the photoresist layer is reduced, and this is under development.

A dummy modules with thinned parts has been assembled. This module does not allow electrical continuity testing, but X-Ray inspection shows a defect rate(merged bumps, there are no missing bumps) of better than 10-3.

### Sofradir

Five(4") dummy wafers have been thinned by Micropolish in France (4 wafers down to 200 µm, 1 down to 150 µm).

Seven dummy modules have been assembled using these thinned die. The electrical inspection results are reported elsewhere in this document as are the X-Ray inspection results(very few defects).

## Preliminary Production Plan

Our limited results so far indicate that it is feasible to mechanically thin the front-end IC wafers to 150-200 microns. However, we need considerably more experience to assess the actual yield of the process, and to evaluate the tradeoffs between reaching the 150 micron goal and yield.  Mechanical thinning(eg. as done by Okamoto) is a standard industrial process done by robotic machinery, although tape removal(after UV exposure) for these thin wafers has been done by hand, as is inspection and reporting. The thinning capacity in this case if very much larger than our need and the typical turn-around time for a wafer lot can be 3-4 days.  The cost, in large quantities, is about 20 chf per wafer(6").  So far we have had positive experience with two vendors: Okamoto in the U.S. and Micropolish in France. Two(or more) vendors would reduce the risk in production but is not required to meet the production schedule.

# Endnotes

Tru-Si Technologies, 657 Patoria Ave., Sunnyvale CA 94086. A wafer was thinned by this process. We are not currently considering this process for production for the following reasons: cost, it requires first mechanical grinding to about 300 microns thickness for most economical results and the wafer temperature can get close to the melting point of Indium. We intend to follow the development of this method of wafer thinning in case it becomes more practical, since it is a non-contact process well suited to bumped wafers.

GDSI, 247 Humboldt Court, Sunnyvale CA 94089.

"Results on 0.7% Thick Pixel Modules for the ATLAS Detector", P. Netchaeva et al, submitted to the Proceedings of the Pixel 2000 Conference.

Okamoto Corporation, 2370 Owen St. Santa Clara CA 95054.

Furakawa SP-589 or similar.