Concept for Integrated Mechanical/Cooling Pixel Supports

The basic concept for all pixel supports is to embed a small diameter cooling tube (2-3 mm OD) in low-density, carbon foam (described in the next session) with high modulus carbon fiber (e.g.  K13D2U) surrounding the foam.  Electrical services may also be embedded in the foam or glued to the surface of the carbon fiber. A cross section (assuming embedded electrical services) of a barrel stave is shown in Figure 1 and the overall stave concept is shown in Figure 2.

Figure 1. Cross section of the general concept for pixel mechanical/cooling supports with embedded electrical services.

A similar concept can be used in disk structures in which the cooling tube is appropriately bent and routed. The nominal choice for the cooling pipe material is titanium, although stainless steel could also be used if titanium proves unworkable.

Figure 2. Example of stave concept with pixel modules on both sides of the stave.

Coupled-layer structures are also possible for the innermost layers. An example is an I-beam structure – see Figure 3(left) for a cross section of the concept and Figure 3(right) for a short prototype. The basic thermal structure is the same as shown above. Very thin carbon-fiber material is used for the web and high-performance fiber (K13D2U) for the facings as before. The same type of foam has been used. A short prototype has been made. Thermal performance measurements have been made and the results are as predicted. Deflection tests validate an FEA model of the structure.

Figure 3. Left: Cross section of a coupled layer concept. Right: end region of a prototype.

Foam Development

The basis of the mechanical supports for pixel modules is a new type of low-density, all-carbon,  thermally-conducting foam being developed by Allcomp, Inc. This light-weight foam is manufactured starting with reticulated vitreous carbon foam material (very low thermal conductivity) that is treated using a proprietary chemical vapor deposition process followed by heat treatment at high temperature. The material is typically made in blocks up to 30cmx30cmx2.5cm and the density of interest for pixel mechanical supports is in the range 0.20-0.25 g/cc. A typical block is shown in Figure 4(left) and the foam structure in Figure 4(right).

Figure 4. (Left) Typical block of foam manufactured by Allcomp, Inc. (Right) Foam microstructure.

The foam is readily machinable into complex shapes. Preliminary measurements of foam properties have been made – see Table 1. The thermal conductivity and mechanical properties depend on the density.  The compressive properties in particular exhibit non-linear behavior. A representative stress-strain curve is shown in Figure 5.

| Property | Value(Unit) |
| --- | --- |
| Density | 0.23 g/cc |
| Initial porosity | 130 pores/inch |
| Thermal conductivity | 30-40 W/m-K |
| CTE | <2 ppm/oC |
| Tensile modulus | 35ksi |
| Tensile strength | 515psi |
| Compressive modulus | 50ksi |
| Compressive strength | 280psi |

Table 1. Representative foam properties.	       Figure 5. Compressive stress vs. strain.

The coolant pipe is glued into a circular channel in the foam using boron-nitride loaded epoxy (Hysol 9396). The BN-Hysol material partially fills the pores of the foam around the pipe as shown in Figure 6.

The CTE of the BN-Hysol filled foam (at 30% BN-Hysol by weight) has been measured as a function of temperature – see Figure 7. Not that the CTE of HYSOL9396 unfilled is about 70 ppm at room temperature.

Figure 6. Cross section of pipe-foam-glue.	Figure 7. CTE of BN-Hysol(30% by weight) foam vs temperature.

Prototype Testing Summary

A variety of prototypes have been fabricated and tested.  The testing has focused primarily on reliability and thermal performance after extensive thermal cycling and irradiation. The results are summarized briefly in this section.

Figure 8. Short prototype stave with Pt-on-silicon heaters (to simulate pixel module heat input).

A number of small stave prototypes (without embedded electrical cables) have been fabricated at LBNL (6 samples) and Allcomp, Inc (2 samples).  Both Ti(2.2mm OD) and stainless steel (2.8mm) OD tubes have been used. These prototypes are about 12cm long, 4 cm wide and 0.5 cm thick.  A photograph of such a prototype (in a holder for thermal IR imaging) is shown in Figure 8. Thin-film, Pt-on-silicon heaters are used to simulate the power load from a pixel module.  These prototypes have been subjected to thermal cycling and irradiation. The thermal performance at each step was measured using water coolant at a flow rate of about 1 l/min. Changes in thermal conductivity or loss of structural integrity would be seen as degraded thermal performance.  Two 1m-long prototypes have also been fabricated, one which is shown in Figure 9. A second 1m prototype (not shown) had the electrical cable embedded in the mid-plane as shown in Figure 2. Thermal performance of these prototypes was evaluated using water coolant and also CO2 cooling.

Figure 9. A 1m stave fabricated at Allcomp, Inc, instrumented at LBNL and tested at LBNL and SLAC. This prototype has an electrical cable glued to the facings and Pt-on-silicon heaters to simulate pixel modules.

A 70cm-long prototype with an embedded active electrical cable was also constructed and tested – see Figure 10.

Figure 10. 70cm-long prototype with active electrical cable embedded in the foam core. The “end-of-stave” region to make electrical connections is on the left, the region of the tabs exiting the stave.

A lengthy series of tests were performed on these staves:

- Short staves

  - Both SS and Ti tubes. 900 thermal cycles (20C<-> -35C), then -70C(dry ice), then               - 175C(LN2), then 150 MRad

  - Different set of staves, 350 thermal cycles (20C<-> -35C)

  - SS tube only, 1 GRad then 250 thermal cycles (20C<-> -35C)

  - Thermal measurements using room temperature water at high flow (1 liter/min) (at both LBNL and Allcomp). Very good agreement between sites.

- 1m staves

  - Thermal measurements using room temperature water at high flow (1 liter/min)(for one at both LBNL and SLAC)

  - CO2 tests (including dozens of thermal cycles to -35 or lower) at SLAC

  - Deflection measurements

- ½ length active stave

  - Thermal measurements using room temperature water at high flow (1 liter/min)(at LBNL)

  - Continuity testing of active cable after assembly(good continuity)

Note that these tests include irradiation to 1 GRad (about the dose expected at the innermost layer of a pixel detector for the SLHC) and a single thermal cycle to nearly LN2 temperature.

A short section of a “bent stave” (20o bend) was manufactured to demonstrate feasibility of such a construction – see Figure 11.

Figure 11. A short section of a bent stave, 20o bend angle.

The key conclusions drawn from these tests are:

- Manufacturing

  - Straightforward but requires attention to details to achieve tight dimensional tolerances

  - Very similar results from two places (LBNL and Allcomp)

  - Bent staves can be made

- After extensive thermal cycling – no change in thermal performance

- After irradiation to 1 GRad. Thermal performance (including module adhesive) degrades by < 10% e.g. by < 1C out of 9-10C total T from bulk fluid T to module surface.

- Operation with CO2 is as expected, good performance

- Comparison of thermal measurements to FEA (see next section) by different people and using different codes – agreement to within about 10% in T with measurements for both water and CO2

Thermal and Stress Analysis

Extensive calculations have been performed to estimate the thermal performance of prototypes with Pt-on-silicon heating elements.  Typical values for the thermal conductivity of the stave components used in the calculations are:

- Foam: Kx=Ky=Kz=30W/mK

- Carbon fiber facing(0-90-0 layup of K13D2U); Kx=219; Ky=110; Kz=0.8W/mK (depends on fiber fraction, in this case 42%)

- Hysol/BN loaded: K =1.0W/mK

- Stainless steel: K=16 and titanium: K=17W/mK

- Adhesive attaching heaters to carbon fiber facings(SE4445): K=0.8W/mK

The thermal properties of the coolant (either water or CO2) were simulated in some detail. A CFD code is used in these thermal studies. Two options were used in defining the coolant convection film coefficient for water: (1) prescribing a fixed value along the tube length; and (2) using the computational features of the code to solve for convection coefficient based on a prescribed inlet coolant tube flow rate.   The fixed convection value was based on Reynolds number of the coolant flow and classical formulas that correlate convection film coefficient with Reynolds number.  The CFD method is more computational tedious and requires sufficient coolant entrance length before the heated region to establish desired flow conditions.

A typical measurement (of the prototype shown in Figure 10 loaded with heaters at one end) is shown in Figure 12(left). The finite element calculation is shown in Figure 12(right)(water cooling). In this case, the agreement between measurement and prediction is very good and in general, agreement between data and predictions within about 10% of the T between the bulk coolant temperature and the average heater temperature is achieved in all cases.

Figure 12. (left) IR thermal image using water cooling and (right) simulation of the expected thermal performance.

FEA static design aspects of the 12cm long stave prototype focused on stresses induced from temperature cycling.  The objective was to predict stresses for critical areas: (1) foam core, (2) thin-walled cooling tube, (3) foam-adhesive filled transition, and lastly (4) composite facing.  No visual damage or change in thermal performance was observed from temperature cycling even to LN2 temperatures.

A purely linear FEA solution pointed to very high stresses in the foam core and the thin-walled stainless steel cooling tube.   Our approach is to include non-linear stress-strain properties for the foam.  This non-linear foam material model results in limited foam stress by describing a pseudo-plastic behavior for the foam.

As the analysis progressed, more foam axial compression and tensile tests were performed, which improved the input to the FEA (stress-strain curves). Tests were also performed on foam-filled with the HYSOL9396 adhesive (filled with BN filler) to determine its elastic properties and thermal expansion as a function of temperature.  This material is used as a transition between the foam core to the cooling tube and to the composite facing.  It simulates adhesive that has been forced into the foam during bonding of the structure.  This new non-linear model of the narrow foam/adhesive region and temperature-dependent CTE values for the stainless steel tube and the silicon heater were included in the analysis.

Adding CTE dependencies for the cooling tube and the foam/adhesive region, coupled with improved foam elastic properties (non-linear) reduced the peak stress in the foam and the cooling tube, both areas of previous concern.  Some conclusions from the analysis to date are:

- Foam surface stress for a 60C temperature change approached, but stayed within the foam compression limit

- Foam stress for 150C (LN2 test) produces a plastic strain of 0.02 for very local array of elements on the foam surface adjoining the adhesive/foam region.  This strain quite possibly would not produce visible damage to the foam.

- Foam peak stress in the very narrow region between the foam and composite facing directly over the cooling tube is almost pure shear.  No foam shear test data exists to compare with the predicted stress.  Since the distance spanned by the foam is ~0.5mm this predicted stress may not be very reliable

- Cooling tube stress (12mil wall in SS tube) has been reduced and appears to be below the yield  limits for the maximum temperature change of 150C.

- Composite facing fiber fraction varied from 43% to 55% depending on whether the material was consolidated in an autoclave or a hydraulic press. CTE for this fiber fraction range varies from -0.76ppm/C to -0.51ppm/C.  Modulus of elasticity (E) also changes as well.  A solution with the lower CTE and lower E did not change the foam stress measurably.

The foam stress along the adhesive interface to the stainless steel cooling tube for a 12 cm prototype is shown in Figure 13 for a 60C temperature change.  The foam surface at tube exit has a minimum principal stress of -1.7MPa (246psi).  Temperature cycling with LN2 is the lower curve and this stress approaches -2.2MPa (319psi), thus the stress has entered the non-linear portion of the foam stress-strain curve.  In spite of this “predicted” situation no outward damage to the foam surface was noted.

Further stress analysis and further testing of all materials will be done.  Foam shear tests will be one area worthy of investigation that would aid in the FEA.

Figure 13: Plot of Minimum Principal Stress, axial along Z-axis, from fine mesh solution of short stave prototype with facing CTE=-0.76ppm/C and for 60ºC and 150ºC temperature change.

Allcomp Inc., 209 Puente Avenue, City of Industry, CA 91746-2304. http://www.allcomp.net/

The density can be adjusted somewhat during the processing. Material with density up to about 0.45 g/cc has been manufactured and is in use in the prototype program for ATLAS upgrade strip stave structures.

CO2 cooling tests were done at SLAC under the direction of M. Oriunno using a so-called “blown system” with coolant temperatures as low as -40C.

Dow Corning SE4445.