ATLAS Pixel Sector and Disk Ring

Carbon-Carbon Plate Specification

April 24, 2000

Draft

Prepreg: 58% (expected  range 57-60 %) by volume P30 fiber and balance phenolic resin. Carbonized and heat treated to achieved performance parameters listed in Table 1.  Panels are to be densified by a CVD carbon process and resin impregnated with RS3 cyanate ester. Scrub plates to remove excess resin.

Panel size:  48.26 cm (19 in.) square or larger.

Number of panels: Preproduction lot of 2 panels. Production lot of minimum 24 panels.

Layup: Quasi-isotropic 8 layers: 0/45/-45/90/s

| Item | Specification | Range or Comment |
| --- | --- | --- |
| Tensile modulus-0( dir. | 158.6 GPa (23 Msi) | Range +/-5% |
| Tensile modulus-90( dir. | 151.7 GPa (22 Msi) | Range +/-5% |
| Tensile strength-0( dir. | 296.4 MPa (43 ksi) | Range +/-5% |
| Tensile strength-90( dir. | 296.4 MPa (43 Msi) | Range +/-5% |
| CTE-0( dir. | -1.2 ppm/K | Range +/-10% |
| CTE-90( dir. | -1.2 ppm/K | Range +/-10% |
| Conductivity Kab-0( dir. | >170 W/mK | Target value: >190 W/mK |
| Conductivity Kc-90( dir. | >170 W/mK | Target value: >190 W/mK |
| Conductivity K transverse | >25 W/mK |  |
| Density | 1.75 g/cc | Range +5/-2% |
| Thickness | 0.406 - 0.457 mm |  |