| Slot # | Wafer Nr. | Wafer-thickness [µm] | Bow [µm] | Warp [µm] | Wafer | Resit | Deep UV exposer [26,5 mW measured at 310nm] | Thin ( |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 20347 W000978 | 559 | -7 | 21 | Monitorwafer with oxidlayer and thin metal structures | 1.Layer 15µm with edge removal 2.Layer 15µm without edge removal | 4min |  |
| 2 | 20348 W001007 | 560 | -2 | 8 | Monitorwafer with oxidlayer and thin metal structures | 1.Layer 15µm with edge removal 2.Layer 15µm without edge removal | 2 min |  |
| 3 | T01 | 701 | 2 | 14 | Monitorwafer with oxidlayer | 1.Layer 15µm with edge removal 2.Layer 15µm without edge removal | 1 min |  |
| 4 | 20119 W001671 | 548 | -11 | 38 | Monitorwafer with oxidlayer | 1.Layer 15µm with edge removal 2.Layer 15µm without edge removal | 0 min | 189 |
| 5 | T02 | 699 | -16 | 34 | Monitorwafer with oxidlayer | 1.Layer 15µm with edge removal 2.Layer 15µm without edge removal | 0 min |  |
| 6 |  |  |  |  |  |  |  |  |
| 7 | 20231 W001813 | 556 | 8 | 20 | Monitorwafer with PbSn Bumps etched and reflowed | 1.Layer 15µm with edge removal 2.Layer 15µm without edge removal | 0 Some speckle interaction with tape | 210 |
| 8 |  |  |  |  |  |  |  |  |
| 9 | 20363 W001341 | 556 | 8 | 23 | Monitorwafer with PbSn Bumps etched and reflowed Dirt/bubbles present | 1.Layer 15µm with edge removal 2.Layer 15µm without edge removal | 0 Some speckle interaction with tape | 210 |
| 10 |  |  |  |  |  |  |  |  |
| 11 | 20364 W001281 | 552 | 1 | 7 | Monitorwafer with PbSn Bumps etched and reflowed Dirt/bubbles present | 1.Layer 15µm with edge removal 2.Layer 15µm without edge removal | 2 No tape interaction | 210 |
| 12 |  |  |  |  |  |  |  |  |
| 13 | 20368 W001241 | 557 | 6 | 20 | Monitorwafer with PbSn Bumps etched and reflowed | 1.Layer 15µm with edge removal 2.Layer 15µm without edge removal | 2 No tape interaction | 210 |
| 14 |  |  |  |  |  |  |  |  |

| Slot # | Wafer Nr. | Wafer-thickness [µm] | Bow [µm] | Warp [µm] | Wafer | Resit | Deep UV exposer [26,5 mW measured at 310nm] |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 15 | 20065 | 690 | -4 | 10 | Monitorwafer with PbSn Bumps as plated Resist not stripped, not etched, not reflowed | Resist as plated No additional Resist | 0 |  |
| 16 |  |  |  |  |  |  |  |  |
| 17 | 20124 W001276 | 553 | -7 | 17 | Monitorwafer with PbSn Bumps as plated Resist not stripped, not etched, not reflowed | Resist as plated No additional Resist | 0 | 203 |
| 18 |  |  |  |  |  |  |  |  |
| 19 | 20127 W001999 | 553 | -10 | 22 | Monitorwafer with PbSn Bumps as plated Resist not stripped, not etched, not reflowed | Resist as plated No additional Resist | 1 | 203 |
| 20 |  |  |  |  |  |  |  |  |
| 21 | 20122 W001429 | 551 | -8 | 20 | Monitorwafer with PbSn Bumps as plated Resist not stripped, not etched, not reflowed | Resist as plated No additional Resist | 1 | 280 |
| 22 |  |  |  |  |  |  |  |  |
| 23 | 20216 W001264 | 550 | -11 | 22 | Monitorwafer with PbSn Bumps as plated Resist not stripped, not etched, not reflowed | Resist as plated No additional Resist | 2 | 280 |
| 24 |  |  |  |  |  |  |  |  |
| 25 | 20121 W001271 | 549 | -16 | 31 | Monitorwafer with PbSn Bumps as plated Resist not stripped, not etched, not reflowed | Resist as plated No additional Resist | 2 | 190 |

# Footnotes

Thickness includes photoresist coating, which is roughly 25 microns.